SPECIFICATIONS FOR ALGAE FLOC

| No | ITEM | SPECIFICATIONS |
| --- | --- | --- |
| 1 | ALGAE FLOC 19s-Flocculants | Typical properties: Liquid polymer blend |
|  |  | Appearance and odour: Clear, orange/yellow liquid |
|  |  | Specific gravity@25ºc:1.175-1.210 |
|  |  | pH(neat):4.0ph units max |
|  |  | Solubility: Soluble in water |
|  |  | Viscosity@ 25ºc:30-100cps |
|  |  | Usage:Flocculant for drinking water |
|  |  | Certification:NSF to ANSI/NSF Standard 60 |
|  |  | Packaging: The product shall be presented in 250kg plastic drums clearly labelled with the following information; Net content, Batch/Lot Number, Name of Manufacturer and Address, Manufacturer and Expiry Dates, Manufacturer’s Quality Assurance Product Test Report |